Photocatalytic decolourisation of textile azo dyes

A)

Teresa M. Miranda1 , Graça M. B. Soares1*, Ana M. F. Oliveira -Campos2, , Martin Kaja3,, Radim Hrdina3 and Oldřich Machalický3

1Departmento de Engenharia Têxtil, Universidade  do Minho, 4800 -058 Guimarães, Portugal

tmiranda@det.uminho.pt; gmbs@det.uminho.pt

2 Centro de Química, IBQF, Universidade do Minho, 4710-320 Braga, Portugal

amcampos@quimica.uminho.pt

3 Department of Organic Technology, University of Pardubice, Studentská 95, Pardubice, Czech Republic

Radim.Hrdina@upce.cz

A)	Keywords

Mordant dyes, Photocatalytic treatment, Oxidation of dyes; Quantum Yield, Decolouration, Actinometry, Polychromatic irradiation

ABSTRACT

Four model dyes were synthesised using classical preparative techniques. They represent the molecular structures frequently used in the production of industrial textile mordant dyes. Dyes decolourisation was developed in a lab-scale thin film photoreactor equipped with a white lamp and quartz tube, in the presence of different semiconductors, such as TiO2, ZnO and Fe2O3. The quantum yields of photochemical degradation were determined.

The contribution of this photocatalytic process to the textile wastewater decolourisation will be discussed.

Introdution

Industrial textile processes generally need very large amounts of clean water to respond to the quality control requirements of the textile products processed

In order to diminish the needs of fresh water and to respect environmental obligations, the concept of water recycling is now being applied. In order to be possible to reuse the water, efficient, strong wastewater treatments are needed to degrade the contaminants such as dyes, surfactants, chelating agents, pH regulators and other compounds. In fact the textile industry uses more than ten thousand different commercial products and more than three thousand are dyes with different molecular structures (chromophores). The major part of these dyes is azo dyes. It is estimated that usually 30-40% of the dye is not fixed on the fibre and this portion is the effluent from the dyeing process.

The textile wastewater is usually treated by different physical (adsorption, filtration, sedimentation) and chemical methods (oxidative mineralization, photochemical degradation) or by a sludge biochemical process. However, the common processes are still ineffective to obtain the complete wastewater effluent mineralization and for this reason the photocatalytic treatment of textile azo dyes is the aim of our presented work.

The photocatalytic treatment in the presence of semiconductors (in this work metal oxides) has been successfully used to oxidise many organic pollutants, which are present in aqueous systems (Xagas et al., 2000). The target of this technology is the complete mineralization of pollutants to harmless compounds - CO2 and H2O. Previous works suggests that this process can mineralise practically any pollutant but the catalyst is one of the key factors.

Our group is interested in the degradation of textile dyes and we chose the combination of different degradation technologies to obtain clean water suitable to be recycled and re-used in the textile processing (Soares et al., 2002, Gonçalves et al., 1999). The main goal of the present work is to compare the mineralization of model dyes in laboratory thin film photo-reactor, equipped with a white lamp and a quartz tube, in the presence of different semiconductors, such as TiO2, ZnO and Fe2O3. The model compounds represent common molecular structures of mordant dyes used in the textile dyeing process. The quantum yields of the photochemical degradation were calculated and compared for two model dyes.

EXPERIMENTAL PART

Preparation of model azo dyes

Dye I (Table I) was prepared by the routine method, the diazotisation of primary aromatic amine and subsequent coupling reaction to an appropriate secondary compound.

The Dye II (Orange II) was purchased from CIBA.

Table I. The set of model dyes

| Dye | I | II |
| --- | --- | --- |
| Structure |  |  |

Photocatalytic treatment

Reagents: The semiconductor TiO2 used in this work was from the corporation DEGUSSA (Degussa P25) with particles 25 nm and a surface area 50 m2g-1.

The semiconductors ZnO and Fe2O3 were purchased from RIEDEL DE HAEN (technical grade).

Equipment: The photochemical reaction was done in the thin film photoreactor TFQ15/TFB15 (Photochemical reactors LTD, UK) (Fig. 1). This photochemical reactor is equipped with the white lamp (model 3028, 15W) (spectral emission is on the Fig. 2) and with the protective quartz tube.

UV-visible spectra were determined on a Hitachi U-2000 UV spectrophotometer.

Preparation of ferrioxalate actimometer - K3Fe(C2O4)3.3H2O

Actinometer was prepared as described in Hatchard and co-workers (Hatchard 1956), but using FeCl3 instead Fe2(SO4)3  The obtained ferrioxalate is more pure than if prepared by the classical method, because KCl formed from FeCl3 is much more soluble in the water (~20 mass %) then K2SO4 formed from Fe2(SO4)3 (~5 mass %).

Figure 1. Laboratory photochemical thin film reactor TFQ15/TFB15

Figure 2. Spectral emission of white lamp (model 3028)

Photodegradation procedure

Photochemical oxidation was carried out in water with the total reaction time 240 minutes (the time of irradiation), where different quantities of semiconductor (TiO2 or ZnO or Fe2O3) were dispersed and different amounts of model dye were dissolved. After adjusting the pH to the value 12 with 6M NaOH the reaction mixture was placed in the photochemical thin film reactor. Aliquots (2.5 cm-3) were taken during the irradiation at known intervals, the semiconductor powder was separated by centrifugation from the sample and the absorption (A, at the beginning of irradiation A0) of the solution was measured.

Results and discussion

The photocatalytic treatment of wastewater with a polychromatic source, where a dye is dissolved and a semiconductor is presented, has very complicated mathematical description (kinetic model).

In this model we assume that:

·	the dye (D) is completely dissolved in water and TiO2 (T) is in the form of very fine dispersion;

·	the radiation is switch on after intensive stirring and after formation of adsorption equilibrium on the TiO2 surface (Langmuir adsorption isotherm), where complex dye-TiO2 (TD) comes into existence;

·	there is no transport energy from exited dye (dissolved or adsorbed) to the semiconductor;

·	the photochemical reaction does not occur if TiO2 is not present in the batch.

The following equations 1-9 can express the photochemical destruction of a dye on the surface of TiO2 in the water.

Adsorption process (before irradiation)

| Process | Reaction rate |  |
| --- | --- | --- |
| T + D ® TD (resp. Dadsorbed) | k1[T][D] | (1) |
| TD ® T + D | k-1[TD] | (2) |

A)	Photochemical ineffective light absorption

| D + hn ® D* | IabsD | (3) |
| --- | --- | --- |
| D* ® D + D | kD[D*] | (4) |

| TD (resp. Dadsorbed) + hn ® TD* | IabsTD | (5) |
| --- | --- | --- |
| TD* ® TD + D | kTD[TD*] | (6) |

Photochemical process

| T + hn ® T* | IabsT | (7) |
| --- | --- | --- |
| T* ® T + D | kT[T*] | (8) |
| T* + D ® Prod | kR[T*][D] | (9) |

IabsX   is the intensity of absorption of monochromatic light by the compound X

(mole of photons.s-1.dm-3) ;

[X]      is the actual concentration of compound X in the reaction time t

(mol.dm-3);

Prod   is the primary product of photochemical reaction.

The reaction rate (r) of dye destruction is described by equation 10,

where  K1 = k1/k-1,  c0T = [T]  + [TD],  c0D = [D]  + [TD], and

The reaction rate at the beginning of irradiation (r(0)) is then described by the equation 11.

The monochromatic light is absorbed by the complex TD (eTD), TiO2 (eT) and the dissolved dye D (eD) in the reaction mixture (equation 12), where L is the optical length.

Atotal(0) = (eTD.[TD]0 + eD.[D]0 +eT.[T]0).L               (12)

Total absorbed light is given by the equation (13), where I0 is the intensity of incident light (mole of photons.s-1.dm-2), S is the area of illumination (dm2), V is the reaction volume (dm3).

Usually we can assume, that all the light is absorbed in the reaction mixture (Atotal(0) > 2) at the beginning of illumination (equation 14).

This simplification can not be done for the thin film photoreactor. The equation 15 describes the initial absorption of light by the semiconductor and the initial reaction rate is given by the equation 16, where j0 is the reaction constant.

Theoretical relation between r(0) and [D]0 and can be predicted , where r(0) = 0 if [D]0 = 0

and r(0) = 0 if [D]0 ® ¥. The function 16 has maximum (rmax, [D]0opt), which can be computed from the equation 17, where b = kT K1 + kR K1 c0T ,   c = eD - eTD ,  d = eT [T]0 + eTD c0D .

The equation (16) is valid for every monochromatic light l and for the polychromatic light can be integrated (equation 18), where we define the initial integral constant (F0) and also the total initial reaction rate of dye destruction (R0). The source of light we suppose to be a medium-pressure mercury lamp with “line” emission spectrum.

The function 11 (rr0) and the maximum location (rr0max, [D]0opt) depends at the wavelength and the intensity of monochromatic light. The integral reaction rate for the polychromatic source RR0 is the summation of rr0l (RR0 = å rr0l). The functional maximum (RR0max) for some concentration of dissolved dye [D]0opt can be predicted, if we know all experimental (s,V,I0l), physical (eD,T,TD) and chemical constants (K1,kd,r).

From the kinetic model we can see, that predicted velocity of a dye oxidation strongly depends on the affinity of the dye to the semiconductor surface.

Secondly, the concentration proportion between the dye and the semiconductor should be carefully adjusted to obtain the maximum velocity of the photo destruction

DETERMINATION OF RADIATION INTENSITIES

The photocatalytic treatment was carried out in thin film photochemical reactor TFQ15/TFB15 equipped with polychromatic source (white lamp, model 3028).For the presented study (calculation of quantum yields, respectively efficiencies) was then necessary to determine the incident radiation intensities.

The total emission (in the spectral range 350-700 nm) was then 6.14E-06 einstein.s-1.

DETERMINATION OF QUANTUM EFFICIENCIES

The quantum yields, more exactly quantum efficiencies (we can not consider, that all incident light was absorbed) of the photochemical destructions were determined for model dye I and TiO2 or ZnO or Fe2O3 as the semiconductor.

Figure 3. Decolourisation of dye I and Orange II (1mM of dye and 1.17gL-1of semiconductor )

The calculated quantum efficiencies of the photochemical reactions (photocatalytic treatment of the dye I and Orange II, figure 3) are shown in the table II.

From our previous work it is known that the reaction rate is maximum at pH in the range 12-13, and thus all experiments were carried out at pH 12. The example of the kinetic is on the figure 3.

Table II. Quantum efficiencies of model dyes (1mM of dye I and 1.17gL-1of semiconductor )

|  | Quantum efficiency (%) |
| --- | --- |
| Semiconductor | Dye I | Orange II |
| TiO2 |  |  |
| ZnO |  |  |
| Fe2O3 |  |  |

From the obtained results we can see, that the quantum yield (efficiency) of the photochemical destruction on the semiconductor surface is very low. The reason for this low quantum yield is in very low affinity of the dye to the semiconductor surface (this conclusion is in accordance with the kinetic model).

Conclusions

It is observed that the ZnO is the most efficient semiconductor in the photocatalytic process for the two dyes studied, possibly due to their stronger adsorption to its surface. However the structure of the dye may strongly influence the quantum yield of photodegradation. Further examples will be needed to confirm this dependence.

The semiconductors that were used in this study have low affinity to water-soluble dyes (anionic acid, direct and reactive dyes), which causes low quantum yield of primary oxidation of dye molecules. For this reason we intend to modify the semiconductor surface, especially to form "large surface with positive charges", where the photochemistry of model and commercial dyes are studied. These anionic dyes have higher affinity to modify semiconductor and higher quantum yield of primary oxidation is obtain. This work is underway.

In future, the conjugation of the photocatalytic and enzymatic degradation of textile dyes will be studied.

References

C.G.Hatchard, C.A.Parker, Proc. Roy. Soc. (London), A235, 518, 1956)

Gonçalves, M.T.S., Oliveira-Campos, A.A. M.F, Pinto, EMMS, Plasência, P.M.S and Queiroz, M.J.R.P.(1999). Photochemical treatment of solutions of azo dyes containing TiO2 . Chemosphere, Vol.39, Nº5, 781-786.

Soares, GMB., Amorim, MTP., Oliveira-Campos, AM., Hrdina R., Costa-Ferreira, M. (2002) Specificity of phenolic disazo compounds in relation to transformation by laccase. Enzyme Microb. Technol 30, 607-612.

Xagas, A.P., Bernard, M.C., Hugot-Le Goff, A. , Spyrellis, N., Loizos, Z. and Falaras, P. (2002)

Surface modification and protosensitisation of TiO2 nanocrystalline films with ascorbic acid

Journal of photochemistry and Photobiology A:Chemistry 132, 115-120.

Acknowledgements

NATO SCIENCE FELLOWSHIPS, GRANT N. ICCTI 004489 07/08 02